**Ru foil**

05-06-2021 – …../..

PETRA III Extension Beamline P65

XAS CONTINUOUS MODE

Chart, line chart

Description automatically generated

E0 = **22117** eV, Edge step = **1.6**, Pre-edge = -150 to -30 eV, Normalization = 50 to 900 eV

Chart

Description automatically generated kw = 2

Chart, line chart

Description automatically generated FT k range = 2.3 – 15.4 Å-1